The use of isotopic tracing to study the formation of the alteration layer on corroded glass

Rencz, E.A.*(1), Hand, R.J.(1), Neeway, J.J.(2), Pearce, C.I.(2),  Zhu, Z.(2), Harrison, M.T. (3) & Thorpe, C.L.(1).

(1) ISL, School of Chemical, Materials & Biological Engineering, University of Sheffield, S1 3JD, UK

(2) Pacific Northwest National Laboratory, Richland, WA, USA.

(3) United Kingdom National Nuclear Laboratory, Central Laboratory, Sellafield, Seascale, Cumbria, CA20 1PG, UK

Abstract

Vitrification is used to immobilize radioactive elements from spent fuel reprocessing and is increasingly being considered for other waste streams. It is important to study the altered layer that forms on the glass surface when it comes in contact with water to understand their long-term durability in a disposal context. The effect that the silica concentration has on the alteration layer was studied to see if the formed layer is derived primarily from the glass or the solution. ISG and SON68 glasses were altered in a flowthrough system with six different Si concentrations with a consistent 29Si/28Si ratio enriched in 29Si. Time-of-Flight Secondary Ion Mass Spectrometry was used to compare the isotope ratio in the alteration layers and ascertain the contribution from solution derived silica. A concentration dependent solution contribution was observed in all samples with the alteration layers containing 29Si.